Ferrite magnet

Ferrite magnets are sintered permanent magnets composed of Barium or Strontium Ferrite. This class of magnets, aside from good resistance to demagnetization, has the popular advantage of low cost.
Ferrite magnets are very hard and brittle, and require specialized machining techniques. Moreover, they should be machined in an unmagnetized state. We are equipped to machine these materials to specifications.

Temperature Effects 

Up to about 840 F, changes in magnetization are largely reversible, while changes between 840 F and 1800 F are re-magnetizable. For all Ferrite magnets, the degradation of magnetic properties is essentially linear with temperature. At 350 F, about 75% of room temperature magnetization is retained, and at 550 F, about 50% is retained.

Common Applications for Ferrite Magnets

Ferrite magnets are widely used in motors, magnetic couplings, for sensing, loudspeakers, holding-magnet systems, crafts, magnetic therapy, novelties, and toys. 

Typical Magnetic Performance for Sintered Ferrite

1. Mostly Used national standard - SJ285-77 permanent ferrite magnet standard 
2.Chinese standard -sj/T10410 2000 permanent ferrite magnet standard 
3.USA standard - permanent ferrite magnet industry standard of USA 
4.The standard from International Electronics Committee(IEC404-8-1)

- Magnetic Properties

Mostly Used national standard - SJ285-77 permanent ferrite magnet standard

| Grade | Value(min/typical in our factory) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Br |  | Hcb(BHC) |  | Hcj(IHC) |  | (BH)max |  |
|  | MT | KG | KA/m | Koe | KA/m | KOe | Kj/m3 | MGOe |
| Y10T(=C1) | 200-218 | 2.00-2.18 | 125-145 | 1.57-1.82 | 210-250 | 2.64-3.14 | 6.5-8.0 | 0.8-1.0 |
| Y25 | 360-370 | 3.60-3.70 | 135-150 | 1.70-1.88 | 140-170 | 1.76-2.14 | 22.5-25.3 | 2.8-3.2 |
| Y30(=C5) | 380-385 | 3.80-3.85 | 191-210 | 2.40-2.64 | 199-220 | 2.50-2.51 | 26.0-28.0 | 3.4-3.7 |
| Y30BH | 380-390 | 3.80-3.90 | 223-235 | 2.80-2.95 | 231-245 | 2.90-3.08 | 27.0-30.0 | 3.4-3.7 |
| Y33 | 410-420 | 4.10-4.20 | 220-235 | 2.77-2.95 | 225-240 | 2.83-3.01 | 31.5-33.0 | 4.0-4.2 |
| Y35 | 400-410 | 4.00-4.10 | 175-195 | 2.20-2.45 | 180-200 | 2.26-2.51 | 30.0-32.0 | 3.8-4.0 |
| C8(=C8A) | 385-390 | 3.85-3.90 | 235-255 | 2.95-3.20 | 242-265 | 3.05-3.33 | 27.8-30.0 | 3.5-3.7 |
| C10 | 400-410 | 4.00-4.10 | 288-300 | 3.62-3.77 | 280-287 | 3.51-3.60 | 30.4-31.9 | 3.8-4.0 |

Chinese standard -sj/T10410 2000 permanent ferrite magnet standard

| Material | Br |  | HcB |  | HcJ |  | (BH)max |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | mT | KG | KA/m | Oe | KA/m | Oe | Kj/m³ | MGOe |
| Y8T | 200-235 | ≥2000 | 125-160 | ≥1570 | 210-280 | 2610 | 6.5-9.5 | ≥0.8 |
| Y22H | 310-360 | ≥3100 | 220-250 | ≥2770 | 280-320 | 3520 | 20.0-24.0 | ≥2.5 |
| Y25 | 360-400 | ≥3600 | 135-170 | ≥1700 | 140-200 | 1760 | 22.5-28.0 | ≥2.8 |
| Y26H-1 | 360-390 | ≥3600 | 220-250 | ≥2512 | 225-255 | 2830 | 23.0-28.0 | ≥2.9 |
| Y26H-2 | 360-380 | ≥3600 | 263-288 | ≥3300 | 318-350 | 4000 | 24.0-28.0 | ≥3.0 |
| Y27H | 370-400 | ≥3500 | 225-240 | ≥2830 | 235-260 | 2950 | 25.0-29.0 | ≥3.1 |
| Y28 | 370-400 | ≥3700 | 175-210 | ≥2200 | 180-220 | 2260 | 26.0-30.0 | ≥3.3 |
| Y28H-1 | 380-400 | ≥3800 | 240-260 | ≥3020 | 250-280 | 3140 | 27.0-30.0 | ≥3.1 |
| Y28H-2 | 360-380 | ≥3600 | 271-295 | ≥3400 | 382-405 | 1800 | 26.0-30.0 | ≥3.3 |
| Y30 | 370-400 | 3.7~4.0 | 175-210 | 2.20~2.64 | 180-220 | 2.26~2.77 | 26.0-30.0 | 3.3~3.8 |
| Y30H-1 | 380-400 | ≥3800 | 230-275 | ≥2890 | 235-290 | 2950 | 27.0-32.5 | ≥3.4 |
| Y30H-2 | 395-415 | ≥3950 | 275-300 | ≥3460 | 310-335 | 3900 | 27.0-32.0 | ≥3.4 |
| Y32 | 400-420 | ≥4000 | 160-190 | ≥2010 | 165-195 | 2070 | 30.0-33.5 | ≥3.8 |
| Y32H-1 | 400-420 | ≥4000 | 190-230 | ≥2390 | 230-250 | 2890 | 34.5-35.0 | ≥4.0 |
| Y32H-2 | 400-440 | ≥4000 | 224-240 | ≥2810 | 230-250 | 2890 | 31.0-34.0 | ≥3.9 |
| Y33 | 410-430 | ≥4100 | 220-250 | ≥2760 | 225-255 | 2830 | 31.5-35.0 | ≥4.0 |
| Y33H | 410-430 | ≥4100 | 250-270 | ≥3140 | 250-275 | 3140 | 31.5-35.0 | ≥4.0 |
| Y34 | 420-440 | ≥4200 | 200-230 | ≥2510 | 205-235 | 2580 | 32.5-36.0 | ≥4.1 |
| Y35 | 430-450 | ≥4300 | 215-239 | ≥2700 | 217-242 | 2730 | 33.1-33.2 | ≥4.2 |

USA standard - permanent ferrite magnet industry standard of USA

| Material | Br |  | HcB |  | HcJ |  | (BH)max |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | mT | KG | KA/m | KOe | KA/e | KOe | kj/m³ | MGOe |
| C1 | 230 | 2.30 | 148 | 1.860 | 258 | 3.50 | 8.36 | 1.05 |
| C5 | 380 | 3.80 | 191 | 2.400 | 199 | 2.50 | 27.00 | 3.40 |
| C7 | 340 | 3.40 | 258 | 3.230 | 318 | 4.00 | 21.90 | 2.75 |
| C8(=C8A) | 385 | 3.85 | 235 | 2.950 | 242 | 3.05 | 27.80 | 3.50 |
| C8B | 420 | 4.20 | 232 | 2.913 | 236 | 2.96 | 32.80 | 4.12 |
| C9 | 380 | 3.80 | 280 | 3.516 | 320 | 4.01 | 26.40 | 3.32 |
| C10 | 400 | 4.00 | 288 | 3.617 | 280 | 3.51 | 30.40 | 3.82 |
| C11 | 430 | 4.30 | 200 | 2.512 | 204 | 2.56 | 34.40 | 4.32 |

The standard from International Electronics Committee(IEC404-8-1)

| Grade | Allowed Value (min/typical) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Br |  | Hcb(BHC) |  | Hcj(IHC) |  | (BH)max |  |
|  | MT | KG | KA/m | KOe | KA/m | KOe | Kj/m³ | MGOe |
| HF8/22 | 200-220 | 2.00-2.20 | 125-140 | 1.57-1.76 | 220-230 | 2.76-2.89 | 6.5-6.8 | 0.8-1.1 |
| HF20/19 | 320-333 | 3.20-3.33 | 170-190 | 2.14-2.39 | 190-200 | 2.39-2.51 | 20.0-21.0 | 2.5-2.7 |
| HF20/28 | 310-325 | 3.10-3.25 | 220-230 | 2.76-2.89 | 280-290 | 3.52-3.64 | 20.0-21.0 | 2.5-2.7 |
| HF22/30 | 350-365 | 3.50-3.65 | 255-265 | 3.20-3.33 | 290-300 | 3.64-3.77 | 22.0-23.5 | 2.8-3.0 |
| HF24/16 | 350-365 | 3.50-3.65 | 155-175 | 1.95-2.20 | 160-180 | 2.01-2.26 | 24.0-25.5 | 3.0-3.2 |
| HF24/23 | 350-365 | 3.50-3.65 | 220-230 | 2.76-2.89 | 230-240 | 2.89-3.01 | 24.0-25.5 | 3.0-3.2 |
| HF24/35 | 360-370 | 3.60-3.70 | 260-270 | 3.27-3.39 | 350-360 | 4.40-4.52 | 24.0-25.5 | 3.0-3.2 |
| HF26/16 | 370-380 | 3.70-3.80 | 155-175 | 1.95-2.20 | 160-180 | 2.01-2.26 | 26.0-27.0 | 3.2-3.4 |
| HF26/18 | 370-380 | 3.70-3.80 | 175-190 | 2.20-2.39 | 180-190 | 2.26-2.39 | 26.0-27.0 | 3.3-3.4 |
| HF26/24 | 370-380 | 3.70-3.80 | 230-240 | 2.89-3.01 | 240-250 | 3.01-3.14 | 26.0-27.0 | 3.3-3.4 |
| HF26/26 | 370-380 | 3.70-3.80 | 230-240 | 2.89-3.01 | 260-270 | 3.27-3.39 | 26.0-27.0 | 3.3-3.4 |
| HF26/30 | 385-395 | 3.85-3.95 | 260-270 | 3.27-3.39 | 300-310 | 3.77-3.89 | 26.0-27.0 | 3.3-3.4 |
| HF28/26 | 385-395 | 3.85-3.95 | 250-265 | 3.14-3.33 | 260-275 | 3.27-3.45 | 28.0-30.0 | 3.5-3.8 |
| HF28/28 | 385-395 | 3.85-3.95 | 260-270 | 3.27-3.39 | 280-290 | 3.50-3.60 | 28.0-30.0 | 3.5-3.8 |
| HF30/26 | 395-405 | 3.95-4.05 | 250-260 | 3.14-3.33 | 260-270 | 3.27-3.39 | 30.0-31.5 | 3.8-3.9 |
| HF32/17 | 410-420 | 4.10-4.20 | 160-180 | 2.01-2.26 | 165-175 | 2.07-2.20 | 32.0-33.0 | 4.0-4.1 |
| HF32/22 | 410-420 | 4.10-4.20 | 215-225 | 2.70-2.83 | 220-230 | 2.76-2.89 | 32.0-33.0 | 4.0-4.1 |
| HF32/25 | 410-420 | 4.10-4.20 | 240-250 | 3.01-3.14 | 250-260 | 3.14-3.27 | 32.0-33.0 | 4.0-4.1 |

- Physical Properties

Physical Properties of Hard Ferrite

| Parameters | Mark | Unit | Values | Remark |
| --- | --- | --- | --- | --- |
| Recoil Permeability | rec | Gs/Oe | 1.05-1.3 |  |
| Curie Temperature | Tc | ℃ | ≥450 |  |
| Temp. Coefficient of Magnetic Induction | A(Br) | ℃-1 | -0.2% | 0-100℃ |
| Temp. Coefficient of Inturensic Coerrice Induction | A(Hcj) | ℃-1 | -0.2-0.5% | 0-100℃ |
| Density | d | G/cm3 | 4.6-5.0 |  |
| Specific Resistance |  | Ω.cm | ≥106 |  |
| Coefficient of Thermal Expansion | A | ℃-1 | 7-15X10-6 |  |
| Hardness | HV | -- | 480-580 |  |

Ningbo Awork Magnetic Technology Co., LTD. 

Add: Hongdu Road, Jiangbei District, Ningbo of China
Postcode: 315033
Tel: 0086 135 8691 2623
Fax: 0086 574 8739 2649
Email:    Connie: connie.magnets@awork-magnet.com    
        Jane:   Jane.magnets@awork-magnet.com  
         Maria:   maria.magnets@gmail.com
            Nicole:  magnets1017@hotmail.com
Http :     http://www.awork-magnet.com