NdFeb Magnet

Neodymium Iron Boron Magnet Materials --Sintered NdFeB Magnets
Sintered NdFeB magnet is the most permanent magnet in the contemporary. Due to it have good remanence, coercivity and high performance, sintered NdFeB magnet have best magnetic, can support about 640 times of its weight. Now it have been widely used in electronics, electrical, mechanical, medical equipment and others. 

High Energy Density for NdFeB magnet, that can use in modern industry and electronic technology, so that the instrumentation, auto, electric, magnetic separation equipment can change to smaller, lighter, thinner

Involving the sintering of power compacts under vacuum
1、Ginding and slicing possible
2、Very reactive with moisture and oxygen
3、Coasting may be applied depending on the expected enviroment
Application : applied to various electronic motors,engineering equipment,medical equipment ,audio apparatus, and household appliances.

- Magnetic Properties

Typical Magnetic Performance for Sintered NdFeB Magnet

| grade | Remanence Br |  | Coercive force Hcb |  | Intrinsic Coercive force Hcj |  | Maximum Energy (BH)max |  | Tw. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | KGs | T | KOe | KA/m | KOe | KA/m | MGOe | KJ/m3 | (℃) |
| N30 | 10.8-11.2 | 1.08-1.12 | ≥10.00 | ≥796 | ≥12 | ≥ 955 | 28-31 | 223-246 | ≤80 |
| N33 | 11.3-11.7 | 1.13-1.17 | ≥10.50 | ≥836 | ≥12 | ≥ 955 | 31-33 | 247-263 | ≤80 |
| N35 | 11.7-12.1 | 1.17-1.21 | ≥10.80 | ≥860 | ≥12 | ≥ 955 | 33-35 | 263-279 | ≤80 |
| N38 | 12.2-12.6 | 1.22-1.26 | ≥11.30 | ≥900 | ≥12 | ≥ 955 | 36-38 | 287-303 | ≤80 |
| N40 | 12.5-12.8 | 1.25-1.28 | ≥11.40 | ≥908 | ≥12 | ≥ 955 | 38-40 | 303-318 | ≤80 |
| N42 | 12.8-13.2 | 1.28-1.32 | ≥11.50 | ≥915 | ≥12 | ≥ 955 | 40-42 | 326-342 | ≤80 |
| N45 | 13.2-13.7 | 1.32-1.37 | ≥11.60 | ≥924 | ≥12 | ≥ 955 | 43-45 | 342-358 | ≤80 |
| N48 | 13.7-14.2 | 1.37-1.42 | ≥11.60 | ≥923 | ≥12 | ≥ 955 | 46-48 | 367-383 | ≤80 |
| N50 | 14.1-14.5 | 1.41-1.45 | ≥10.00 | ≥796 | ≥11 | ≥ 875 | 48-50 | 383-398 | ≤80 |
| N30M | 10.8-11.2 | 1.08-1.12 | ≥10.00 | ≥796 | ≥14 | ≥1114 | 28-31 | 223-246 | ≤100 |
| N33M | 11.3-11.7 | 1.13-1.17 | ≥10.50 | ≥836 | ≥14 | ≥1114 | 31-33 | 247-263 | ≤100 |
| N35M | 11.7-12.0 | 1.17-1.20 | ≥10.90 | ≥868 | ≥14 | ≥1114 | 33-35 | 263-279 | ≤100 |
| N38M | 12.2-12.6 | 1.22-1.26 | ≥11.30 | ≥900 | ≥14 | ≥1114 | 36-38 | 287-303 | ≤100 |
| N40M | 12.6-12.9 | 1.26-1.29 | ≥11.60 | ≥924 | ≥14 | ≥1114 | 38-40 | 303-318 | ≤100 |
| N42M | 12.9-13.2 | 1.29-1.32 | ≥12.00 | ≥955 | ≥14 | ≥1114 | 40-42 | 326-342 | ≤100 |
| N45M | 13.3-13.5 | 1.33-1.35 | ≥12.20 | ≥971 | ≥14 | ≥1114 | 43-45 | 342-358 | ≤100 |
| N48M | 13.8-14.0 | 1.38-1.40 | ≥12.90 | ≥1027 | ≥14 | ≥1114 | 46-48 | 367-383 | ≤100 |
| N30H | 10.8-11.2 | 1.08-1.12 | ≥10.00 | ≥794 | ≥17 | ≥1353 | 28-30 | 223-239 | ≤120 |
| N33H | 11.4-11.7 | 1.14-1.17 | ≥10.50 | ≥836 | ≥17 | ≥1353 | 31-33 | 247-263 | ≤120 |
| N35H | 11.7-12.0 | 1.17-1.20 | ≥10.90 | ≥868 | ≥17 | ≥1353 | 33-35 | 263-279 | ≤120 |
| N38H | 12.2-12.6 | 1.22-1.26 | ≥11.30 | ≥900 | ≥17 | ≥1353 | 36-38 | 287-303 | ≤120 |
| N40H | 12.6-12.8 | 1.26-1.28 | ≥11.60 | ≥824 | ≥17 | ≥1353 | 38-40 | 303-318 | ≤120 |
| N42H | 12.8-13.0 | 1.28-1.30 | ≥12.00 | ≥955 | ≥17 | ≥1353 | 40-42 | 326-342 | ≤120 |
| N45H | 13.3-13.5 | 1.33-1.35 | ≥12.20 | ≥971 | ≥17 | ≥1353 | 43-45 | 342-358 | ≤120 |
| N30SH | 10.8-11.2 | 1.08-1.12 | ≥10.10 | ≥804 | ≥20 | ≥1595 | 28-30 | 223-239 | ≤150 |
| N33SH | 11.4-11.7 | 1.14-1.17 | ≥10.60 | ≥844 | ≥20 | ≥1595 | 31-33 | 247-263 | ≤150 |
| N35SH | 11.7-12.0 | 1.17-1.20 | ≥11.00 | ≥876 | ≥20 | ≥1595 | 33-35 | 263-279 | ≤150 |
| N38SH | 12.2-12.5 | 1.22-1.25 | ≥11.40 | ≥908 | ≥20 | ≥1595 | 36-38 | 287-303 | ≤150 |
| N40SH | 12.5-12.7 | 1.25-1.27 | ≥11.80 | ≥939 | ≥20 | ≥1595 | 38-40 | 303-318 | ≤150 |
| N42SH | 12.8-13.0 | 1.28-1.30 | ≥12.00 | ≥955 | ≥20 | ≥1595 | 40-42 | 326-342 | ≤150 |
| N45SH | 13.3-13.5 | 1.33-1.35 | ≥12.20 | ≥971 | ≥20 | ≥1595 | 43-45 | 342-358 | ≤150 |
| N28UH | 10.4-10.8 | 1.04-1.08 | ≥ 9.80 | ≥780 | ≥25 | ≥1990 | 26-28 | 207-223 | ≤180 |
| N30UH | 10.8-11.2 | 1.08-1.12 | ≥10.10 | ≥804 | ≥25 | ≥1990 | 28-30 | 223-239 | ≤180 |
| N33UH | 11.3-11.5 | 1.13-1.15 | ≥10.60 | ≥844 | ≥25 | ≥1990 | 31-33 | 247-263 | ≤180 |
| N35UH | 11.7-11.9 | 1.17-1.19 | ≥11.00 | ≥876 | ≥25 | ≥1990 | 33-35 | 263-279 | ≤180 |
| N38UH | 12.2-12.5 | 1.22-1.25 | ≥11.40 | ≥908 | ≥25 | ≥1990 | 36-38 | 287-303 | ≤180 |
| N40UH | 12.5-12.7 | 1.25-1.27 | ≥11.80 | ≥939 | ≥25 | ≥1990 | 38-40 | 303-318 | ≤180 |
| N42UH | 12.8-13.0 | 1.28-1.30 | ≥12.00 | ≥955 | ≥25 | ≥1990 | 40-42 | 326-342 | ≤180 |
| N28EH | 10.4-10.8 | 1.04-1.08 | ≥ 9.80 | ≥780 | ≥30 | ≥2388 | 26-28 | 207-223 | ≤200 |
| N30EH | 10.8-11.2 | 1.08-1.12 | ≥10.10 | ≥804 | ≥30 | ≥2388 | 28-30 | 223-239 | ≤200 |
| N33EH | 11.3-11.5 | 1.13-1.15 | ≥10.60 | ≥844 | ≥30 | ≥2388 | 31-33 | 247-263 | ≤200 |
| N35EH | 11.7-11.9 | 1.17-1.19 | ≥11.00 | ≥876 | ≥30 | ≥2388 | 33-35 | 263-279 | ≤200 |
| N28AH | 10.4-10.8 | 1.04-1.08 | ≥ 9.80 | ≥780 | ≥35 | ≥2785 | 26-29 | 207-231 | ≤220 |
| N30AH | 10.8-11.2 | 1.08-1.12 | ≥10.10 | ≥804 | ≥35 | ≥2785 | 28-31 | 223-246 | ≤220 |
| N33AH | 11.3-11.7 | 1.13-1.17 | ≥10.30 | ≥820 | ≥35 | ≥2785 | 31-33 | 247-263 | ≤220 |
| N35AH | 11.7-12.1 | 1.17-1.21 | ≥10.80 | ≥860 | ≥35 | ≥2785 | 31-35 | 247-279 | ≤220 |

Note: Curie temperature and temperature coefficient are for reference only, but not as inspection base.

- Physical Properties

Physical Properties of Sintered NdFeB:

| Temp.Coeff.of Br | -0.11%/℃ | Temp.Coeff.of Hc | -0.60%/℃ |
| --- | --- | --- | --- |
| Density | 7.4-7.6g/cm3 | Electrical Resistivity | 114μΩ..cm |
| Vickers Hardness: | 600Hv | Flexural Resistivity | 25kg/mm |
| Tensile Strength: | 8.0Kg/mm2 | Coeff. Of Thermal Expansion | 4X10-6/℃ |
| Specific Heat | 0.12Kcal/Kg | Thermal Conductivity | 7.7kcal/[m.h.℃] |
| Young’s Modulus | 1.6X10[11]N/m2 | Rigidity | 0.64N/m2 |
| Poisson’s Ratio | 0.24 | Compressibility | 9.8x10-12m2/N |
| Curie Temperature | 310-340℃ |  |  |

- Surface coating

All coating meets ROHS standard’s requirements

| plating type | plating thickness | color | SST test(hour) | PCT(hour) |
| --- | --- | --- | --- | --- |
| Ni-Cu-Ni | 10-30 | Bright silver | ≥96 | ≥48 |
| Zinc | 5-10 | Dark silver | ≥48 |  |
| Epoxy | 10-30 | black | ≥96 | ≥24 |

We also supply the parylene coating, phosphate treatment based on customer’s request

Ningbo Awork Magnetic Technology Co., LTD. 

Add: Hongdu Road, Jiangbei District, Ningbo of China
Postcode: 315033
Tel: 0086 135 8691 2623
Fax: 0086 574 8739 2649
Email:    Connie: connie.magnets@awork-magnet.com    
        Jane:   Jane.magnets@awork-magnet.com  
         Maria:   maria.magnets@gmail.com
            Nicole:  magnets1017@hotmail.com
Http :     http://www.awork-magnet.com